


                      

COLOR PANEL PROCESS: BT 64/25

CUSTOMER          	:   COTSWOLD
WOOD TYPE		:   OAK + VENEER OAK
PAINT SYSTEM 	:   PU
PRODUCT    		:   INDOOR  FURNITURE                                           Sheen 	               :   20% ± 5%                                   DATE: 07/07/2026
	Process
	Chemicals used &
application steps
	Ratio
	Methods and
equipment used
	Drying time

	* Sanding: Before being painted, the product surface must be treated with sandpaper #240, and defects must be filled to meet requirements (smooth, no rough streaks...)

	1- Color Stain
	Stain BT 64/25
	
	Spray with spray gun
	30 minutes

	2- Spray PU Sealer FD 0212
	PU Sealer FD 0212
PU Hardener 0707 B
PU Primer Thinner
	4
1
2.83 
	Spray 2 passes evenly with a spray gun to wet the surface
	2 → 3 hours, sanding #320
(PU Primer mixed with hardener should be used within 2 to 3 hours)

	3- Color Glaze
	Color Glaze BT 64/25
	
	Brushing
	45→60 minutes

	4- Spray PU Sealer FD 0212
	PU Sealer FD 0212
PU Hardener 0707 B
PU Sealer Thinner
	4
1
2.83 
	Spray 2 passes evenly with a spray gun to wet the surface
	2 → 3 hours, sanding #320
(PU Primer mixed with hardener should be used within 2 to 3 hours)

	5- Color Glaze
	Color Glaze BT 64/25
Glaze Thinner
	1
2
	Spray with spray gun → brush according to sample
	45→60 minutes

	6- Spray PU Sealer FD 0212
	PU Sealer FD 0212
PU Hardener 0707 B
PU Sealer Thinner
	4
1
2.83 
	Spray 2 passes evenly with a spray gun to wet the surface
	2 → 3 hours, sanding #320
(PU Primer mixed with hardener should be used within 2 to 3 hours)

	7-
	Color Stain
	Stain BT 64/25
	
	Spray evenly with spray gun according to sample
	30 minutes

	
	Touch-up Color Glaze
	Color Glaze BT 64/25
	
	Brush according to sample
	45→60 minutes

	8- PU Topcoat 0408 ABR NY 20%
	PU Topcoat 0408 ABR NY 20%
PU Hardener 0707 B
PU Thinner TXXT
	3
1
1.3(1.5
	Spray 2 passes evenly with a spray gun to wet the surface
	After 24 hours, inspect the product; if passed
→ packaging
(PU Gloss mixed with hardener should be used within 2 to 3 hours)


· PAINT APPLICATION NOTES:
- Containers and cans containing paint, colors, solvents... must be tightly closed and stored in a cool, dry place without losing labels.
- Stir the paint and color mixture thoroughly before mixing and painting.
- PU Sealer and PU Topcoat mixed with hardener should be used within 3 to 6 hours.
- Above is the BT 64/25 color sample implementation process and the expected consumption of chemicals used to paint on the sample panels (small specifications). When applicable in actual production, depending on the structure and products produced (tables, chairs, cabinets...), the consumption of chemicals used and the process steps in the production process at the factory should be changed to suit the quality requirements of the sample (paint mixing ratio, color...).
-On hot days, factory temperature ≥ 35°C, humidity ≤ 60%  or humid rain, temperature ≤28°C, humidity ≥ 65%, it is recommended to add Retarder -slow-drying agent -(5-7%) to the Sealer and Topcoat mixture to prevent the paint film from drying too quickly and mold due to weather.
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