#### PAINTING PROCESS GUIDELINES FOR COLOR SAMPLE CARD: BT 64/25

CUSTOMER          	:   COLSWOLD

WOOD TYPE		:   OAK + VENEER OAK

PAINT TYPE 		:   PU

PRODUCT    		:   INDOOR		:                                                GLOSS LEVEL 	               :   20%  5%                                   DATE: 07/07/2026

| ## Step |  | ## Chemicals & Steps & ## Steps | Ratio | Method & Equipment | Drying Time |
| --- | --- | --- | --- | --- | --- |
| *Wood surface sanding :Product surface must be sanded with #240, and defects filled before painting (smooth, no sanding marks…) |  |  |  |  |  |
| 1-Stain |  | Stain BT 64/25 |  | Spray with paint gun | 30 minutes |
| 2- PU Primer FD 0212 |  | PU Primer FD 0212 Hardener PU 0707 B PU Primer Solvent | 4 1 2.83 | Spray 2 passes evenly and wet with paint gun | 2 → 3 hours, sand #320 |
| 3- Glaze color |  | Glaze color BT 64/25 |  | Brush application | 45→60 minutes |
| 4- PU Primer FD 0212 |  | PU Primer FD 0212 Hardener PU 0707 B PU Primer Solvent | 4 1 2.83 | Spray 2 passes evenly and wet with paint gun | 2→ 3 hours, sand #320 |
| 5- Glaze color |  | Glaze color BT 64/25 Glaze Solvent | 1 2 | Spray with paint gun→brush according to sample | 45→60 minutes |
| 6- PU Primer FD 0212 |  | PU Primer FD 0212 Hardener PU 0707 B PU Primer Solvent | 4 1 2.83 | Spray 2 passes evenly and wet with paint gun | 2 → 3 hours, sand #320 |
| 7- | Stain | Stain BT 64/25 |  | Spray with paint gun evenly per sample | 30 minutes |
|  | Glaze touch-up | Glaze color BT 64/25 |  | Brush according to sample | 45→60 minutes |
| 8- PU Topcoat 0408 ABR NY 20% |  | PU Topcoat 0408 ABR NY 20% Hardener PU 0707 B PU Solvent TXXT | 3 1 1.31.5 | Spray 2 passes evenly and wet with paint gun | After 24 hours check product quality → packaging |

- PAINT USAGE NOTES:

# - Paint containers, colorants, solvents... must be tightly sealed and stored in a cool, dry, well-ventilated area. Labels must be preserved.

# - Stir the paint mixture, colorants... thoroughly before mixing and before each application.

# - PU Primer and PU Topcoat mixtures, once the hardener is added, should be used within approximately 2–3 hours.

# - The above is the process for executing color sample BT 64/25 with estimated chemical quantities for sample cards (small scale). When applied

# to actual production, depending on product structure and items (tables, chairs, cabinets...), the chemical quantities and process steps at the factory may be adjusted to meet product quality requirements (paint ratio, color ratio, etc.).

# - On hot sunny days with workshop temperature ≥ 35°C and humidity ≤ 60% (or rainy/humid days with temperature ≤ 28°C and humidity ≥ 65%), it is recommended to add Retarder (5→7%) to the primer and topcoat mixtures to prevent rapid drying and blooming due to weather conditions.