


                      

PAINTING PROCESS GUIDELINES FOR COLOR SAMPLE CARD: BT 64/25

CUSTOMER          	:   COLSWOLD
WOOD TYPE		:   OAK + VENEER OAK
PAINT TYPE 		:   PU
PRODUCT    		:   INDOOR		:                                                GLOSS LEVEL 	               :   20%  5%                                   DATE: 07/07/2026
	Step
	Chemicals & Steps & 
Steps
	Ratio
	Method & 
Equipment 
	Drying Time

	*Wood surface sanding :Product surface must be sanded with #240, and defects filled before painting (smooth, no sanding marks…)

	1-Stain
	Stain  BT 64/25
	
	Spray with paint gun 
	30 minutes

	2- PU Primer FD 0212
	PU Primer FD 0212
Hardener PU 0707 B
PU Primer Solvent
	4
1
2.83 
	Spray 2 passes evenly and wet with paint gun
	2 → 3 hours, sand #320


	3- Glaze color 
	Glaze color BT 64/25
	
	Brush application
	45→60 minutes

	4- PU Primer FD 0212
	PU Primer FD 0212
Hardener PU 0707 B
PU Primer Solvent
	4
1
2.83 
	Spray 2 passes evenly and wet with paint gun
	2→ 3 hours, sand #320


	5- Glaze color 
	Glaze color BT 64/25
Glaze Solvent
	1
2
	Spray with paint gun→brush according to sample
	45→60 minutes

	6- PU Primer FD 0212
	PU Primer FD 0212
Hardener PU 0707 B
PU Primer Solvent
	4
1
2.83 
	Spray 2 passes evenly and wet with paint gun
	2 → 3 hours, sand #320


	7- 
	Stain
	Stain BT 64/25
	
	Spray with paint gun evenly per sample
	30 minutes

	
	Glaze touch-up
	Glaze color BT 64/25
	
	Brush according to sample
	45→60 minutes

	8- PU Topcoat 0408 ABR NY 20%
	PU Topcoat 0408 ABR NY 20%
Hardener PU 0707 B
PU Solvent TXXT 
	3
1
1.31.5
	Spray 2 passes evenly and wet with paint gun
	After 24 hours check product quality  
→ packaging



· PAINT USAGE NOTES:
- Paint containers, colorants, solvents... must be tightly sealed and stored in a cool, dry, well-ventilated area. Labels must be preserved.
- Stir the paint mixture, colorants... thoroughly before mixing and before each application.	
- PU Primer and PU Topcoat mixtures, once the hardener is added, should be used within approximately 2–3 hours.
- The above is the process for executing color sample BT 64/25 with estimated chemical quantities for sample cards (small scale). When applied 
to actual production, depending on product structure and items (tables, chairs, cabinets...), the chemical quantities and process steps at the factory may be adjusted to meet product quality requirements (paint ratio, color ratio, etc.). 
- On hot sunny days with workshop temperature ≥ 35°C and humidity ≤ 60% (or rainy/humid days with temperature ≤ 28°C and humidity ≥ 65%), it is recommended to add Retarder (5→7%) to the primer and topcoat mixtures to prevent rapid drying and blooming due to weather conditions.
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