TECHNICAL TRAINING DOCUMENT

Comparative Guide: NC Solvent-Based vs. Water-Based Coating Systems

────────────────────────────────────────────────────────────────────────────────

**Purpose:** Provide production staff with a clear understanding of the differences between the two coating systems, their proper operation, and the necessary preparations for transitioning from NC to water-based technology.

────────────────────────────────────────────────────────────────────────────────

Part 1: SYSTEM OVERVIEW

1.1. NC (Nitrocellulose) — Solvent-Based System

**What is NC paint?**

A traditional coating that uses **organic solvents** (esters, ketones, aromatic hydrocarbons) as the diluent. When sprayed onto wood, the solvent evaporates, leaving behind a solid paint film.

**Key characteristics:**

• Uses NC thinner (organic solvent) — fast evaporation

• Quick air drying (no oven required)

• Clear, glossy film

• Easy to apply and repair

• Low material cost

**Basic NC process flow:**

Wood cleaning → Sanding → NC Sealer → Sanding →
Stain/color (if needed) → 2nd NC Sealer → Sanding →
NC Topcoat → Inspection → Packaging

1.2. Water-Based Coating

**What is water-based paint?**

A coating system that uses **water** as the primary diluent instead of organic solvents. Acrylic or polyurethane resin particles are dispersed in water using surfactants. When sprayed, water evaporates and the resin particles coalesce to form a continuous film.

**Key characteristics:**

• Diluted with water or specialized diluent

• Requires oven drying or longer drying time vs. NC

• Low odor, environmentally friendly

• Low flammability risk (much safer than NC; cured film is non-flammable)

• Better coverage than NC

• Superior water and chemical resistance

**Basic water-based process flow:**

Wood cleaning → Fine sanding → Anti-grain-raising primer →
Sanding → WB Sealer → Sanding →
WB Stain/color → WB Topcoat →
Oven drying → Inspection → Packaging

────────────────────────────────────────────────────────────────────────────────

Part 2: DETAILED COMPARISON — ADVANTAGES & DISADVANTAGES

2.1. General comparison table

| Criteria | NC (Solvent) | Water-Based |
| --- | --- | --- |
| **Diluent** | NC Thinner (organic solvent) | Water / Specialized diluent |
| **Odor** | Strong, pungent | ✅ Significantly milder |
| **Flammability** | ⚠️ Highly flammable | ✅ Much lower risk (high flash point; non-flammable when fully cured) |
| **Drying time** | Fast (15-30 min/coat) | Slower (30-60 min or oven required) |
| **Oven requirement** | Not needed | ✅ Recommended |
| **Clarity** | ✅ Excellent | Slightly milky when wet, clears upon drying |
| **Coverage** | Moderate (solid content ~30%) | ✅ Better (higher solid content) |
| **Water resistance** | Poor | ✅ Good |
| **Chemical resistance** | Poor | ✅ Good |
| **Yellowing over time** | Yellows after 6-12 months | ✅ Yellows much slower than NC of the same type |
| **Grain raising** | ✅ Minimal (solvent doesn't swell wood) | ⚠️ Significant (water penetrates wood fibers) |
| **Cost** | Lower | ✅ Nearly comparable |
| **Shelf life & storage** | Easy, long shelf life | Short (~6 months), temperature sensitive |
| **Environmental impact** | High (VOC emissions) | ✅ Low |
| **Health & safety** | Poor (inhaling solvent fumes) | ✅ Much safer |

2.2. Advantages of each system

**NC Solvent-Based:**

• [+]  Fast drying — no oven needed, energy saving

• [+]  Easy application — less technical skill required

• [+]  Easy rework — sand and recoat quickly

• [+]  Clear film — excellent stain definition

• [+]  Mature, stable technology — operators are familiar

• [+]  Low material cost

**Water-Based:**

• [+]  Environmentally friendly — low odor, safe for workers

• [+]  Much lower flammability risk than NC — safer storage (coalescing agents have high flash points; cured film is non-flammable)

• [+]  High coverage — fewer coats needed vs. NC

• [+]  Good water and chemical resistance

• [+]  Yellows much slower — suitable for export products

• [+]  Can reduce production time with proper oven drying (with a suitable oven, WB can be faster than NC for the same product)

2.3. Disadvantages & BTChem Solutions

| Disadvantage | BTChem Solution |
| --- | --- |
| ❌ **Slow drying** — depends on oven and weather | 👉 **Sealer S07-2706H + Topcoat B03-241025H** with Diluent BT-08H and Retarder BT-01H for flexible drying control |
| ❌ **Grain raising** — water swells wood fibers | 👉 **Anti-grain-raising Primer BT-1025H** locks wood fibers. Use with fine sanding (320 grit) |
| ❌ **Lower clarity / less vibrant color** — dispersed resin particles scatter light | 👉 **Topcoat B03-241025H** achieves NC-equivalent clarity. **Stain resin BT-0725H** delivers bright, clear colors |
| ❌ **Foaming** — surfactants in water | 👉 BTChem products use **optimized surfactant systems** — reduced foaming. Stir gently, avoid air sparging |
| ❌ **Weather sensitivity** — high humidity slows drying, heat causes flash-off | 👉 **Retarder BT-01H** (for hot weather) + Diluent BT-08H for viscosity stability |
| ❌ **Difficult color matching** — milky when wet, true color appears only when dry | 👉 **Stain resin BT-0725H + water-based dye colors** (Appendix 1) for NC-equivalent color accuracy |
| ❌ **Material cost (historically higher vs. NC)** | 👉 **Now nearly comparable** — price gap has narrowed significantly. Additional savings from higher coverage, fewer coats, reduced labor, and lower fire safety costs |

**Bottom line:** With BTChem's water-based product range — Primer BT-1025H (anti-grain-raising), Sealer S07-2706H, Stain resins BT-0725H/1604H, and Topcoat B03-241025H — most traditional water-based shortcomings have been resolved. Production teams can transition with confidence.

────────────────────────────────────────────────────────────────────────────────

Part 3: CHEMICAL COMPOSITION OF RESINS IN BOTH SYSTEMS

3.1. NC Paint — Nitrocellulose + Alkyd Resin

**Key components:**

• Nitrocellulose (NC):** Produced by nitrating cellulose (cotton linters, wood pulp). This is the primary film-forming resin. NC dissolves completely in organic solvents (NC thinner).

• Alkyd Resin:** Added to improve gloss, flexibility, and adhesion.

**Chemical characteristics:**

• Thermoplastic — dries purely by solvent evaporation, **no chemical curing reaction**

• When solvent evaporates, NC molecules form a film — but it remains soft and can be re-dissolved by fresh solvent

• No chemical cross-linking (curing)** — physical drying only

• Low solids content (typically 18-25% for sealers, up to 30-35% for topcoats — BTChem NC product range; standard market sealers may be lower at 12-20%) — the rest is solvent that evaporates completely

**Practical implication:** NC dries fast but the film is softer, more prone to scratching, and vulnerable to chemical attack. Recoating is easy because fresh solvent partially dissolves the previous layer.

3.2. Water-Based Paint — Acrylic / Polyurethane Dispersion

**Key components:**

• Acrylic Resin:** Nano-sized polymer particles **dispersed** in water using surfactants. As water evaporates, particles approach each other, deform, and coalesce into a continuous film. Acrylic is the standard resin for water-based sealers and topcoats — good clarity, moderate hardness, cost-effective.

• Polyurethane (PUD — Polyurethane Dispersion):** Used in premium water-based lines — harder, more durable, better chemical resistance than acrylic. PUD offers superior abrasion resistance and flexibility.

• Coalescing Agents:** Special organic solvents (Texanol, DPnB...) that soften resin particles to enable film formation at room temperature.

**Chemical characteristics:**

• Thermoplastic or self-crosslinking — dries by water evaporation + particle coalescence

• 1K WB PU** can include a **built-in crosslinker** that activates during film formation for improved durability (e.g., self-crosslinking systems using blocked crosslinkers or DAAM/ADH chemistry — not all 1K WB PU products; depends on formulation)

• 2K WB PU** requires mixing with a **hardener** (isocyanate-based) before application — producing much harder, more chemical-resistant films than NC

• Higher solids content (40-50%)** than NC — thicker film per spray pass

• Once fully dry, the film **does not re-dissolve in water** — unlike NC which remains solvent-soluble

**Practical implication:** WB coatings produce harder, more durable, more chemical-resistant films, but the drying process is more complex — dependent on temperature, humidity, and time for complete particle coalescence.

3.3. Additives Unique to Water-Based Paints (Not Found in NC)

| Additive | Function | Effect |
| --- | --- | --- |
| **Surfactants** | Disperse resin in water, reduce surface tension | ⚠️ Can cause foaming if over-agitated; must be balanced |
| **Coalescing Agents** | Soften resin particles for film formation | ⚠️ Insufficient → cracked film; excessive evaporation → poor coalescence |
| **Defoamers** | Break air bubbles during mixing/spraying | ✅ Necessary; excess → fisheyes, cratering |
| **Biocides** | Prevent bacterial/fungal growth in the can | ✅ Essential — water supports microbial growth |
| **Freeze-thaw stabilizers** | Maintain stability at low temperatures | ✅ Prevents coagulation in cold weather |
| **Leveling agents** | Improve surface smoothness, prevent orange peel | ✅ Enhances surface quality |

**NC paints use a different set of additives** — same functional names (defoamers, leveling agents, flatting agents, driers) but entirely different chemical mechanisms. Unlike water-based additives, NC additives work in a solvent environment: no need for surfactants (resin dissolves directly), no biocides (no water = no microbial growth), no freeze-thaw stabilizers. This mechanism is **more forgiving and stable** — less dependent on temperature, humidity, and pH compared to water-based systems, making NC easier to formulate and more consistent across varying production conditions.

3.4. Why Older Water-Based Systems Had Weaknesses — And How BTChem Products Solve Them

| Old Weakness | Root Cause | BTChem Product Solution |
| --- | --- | --- |
| ❌ **Slow drying** | Water evaporates slower than solvents | 👉 **Sealer S07-2706H + Topcoat B03-241025H** with optimized acrylic system + Diluent BT-08H |
| ❌ **Poor clarity / dull color** | Dispersed particles scatter light | 👉 **Stain resin BT-0725H + Topcoat B03-241025H** — NC-equivalent transparency when dry |
| ❌ **Grain raising** | Water swells wood fibers | 👉 **Anti-grain-raising Primer BT-1025H** locks fibers, prevents water penetration |
| ❌ **Foaming** | Surfactants + agitation | 👉 Optimized BTChem surfactant system + gentle stirring, no air sparging |
| ❌ **Low gloss** | Incomplete particle coalescence | 👉 **Topcoat B03-241025H** for smooth, glossy finish; add 2% TB additive for hardness |
| ❌ **Weather sensitivity** | Water evaporation depends on humidity | 👉 **Retarder BT-01H** (hot weather) + Diluent BT-08H — stable across conditions |

────────────────────────────────────────────────────────────────────────────────

Part 4: NEXT-GENERATION WATER-BASED PRODUCTS — BTCHEM (HÓA KEO BÌNH THẠNH)

**BT Chem** has developed a next-generation water-based product line that overcomes most traditional water-based shortcomings. Below are detailed product specifications and processes.

4.1. Product Lines by Process Type

🔹 Stain System (Wood Dyeing)

**Purpose:** Change wood color while preserving natural grain.

**Products used:**

| Product | Code | Function |
| --- | --- | --- |
| Stain Resin | BT-0725H | Binder for stain color (10-30% of mixture) |
| Diluent | BT-08H | Thinner |
| Dye Colors | Appendix 1 | Yellow, Red, Black, etc. |

**Mixing formula** *(total must equal 100% — adjust within these ranges)*:

Stain Resin BT-0725H: 10-30%
Dye Color:            1-10%  (adjust to target color depth)
Solvent BT-08H:       balance to 100%

*Example: 20% resin + 5% dye + 75% diluent = 100%*

**Improvements vs. older water-based systems:**

• [+]  **Brighter, clearer color** — close to NC system

• [+]  **Reduced grain raising** — thanks to specialized resin + anti-grain primer

• [+]  **Easier application and color adjustment**

• [TIME]  Drying time: **20-30 min** before next step

────────────────────────────────────────────────────────────────────────────────

🔹 Glaze System (Highlighting, Antique Effects)

**Purpose:** Create highlighted grain patterns, antique effects, or enrich wood color.

**Products used:**

| Product | Code | Function |
| --- | --- | --- |
| Glaze | BT-78H (Brown), BT-10H (Black), BT-2506H (Natural) | Color effect |
| Glaze Solvent | BT-25H | Slow drying for easy wipe-off |
| Reducer | 09H | Glaze thinner |
| Supplemental colors | Red BT-01H, Violet BT-01H, Yellow H4G, White Paste 3012H | Color adjustment (<5%) |

**Improvements:**

• [+]  Current water-based sealers now have **sufficient clarity** for beautiful glaze effects

• [+]  Most NC glaze colors can be **replicated in water-based** with no visible difference

• [TIME]  Drying time: **40-60 min**

────────────────────────────────────────────────────────────────────────────────

🔹 Pigment System (Opaque Color)

**Purpose:** Fully cover wood grain, create solid colors.

**Products used:**

| Product | Code | Function |
| --- | --- | --- |
| Oil Sealer | TB-1807H White, TB-2211H | Prevent oil bleed-through from wood |
| Primer | BT-1025H, BT-1025H White | Anti-grain-raising + base coat |
| Pigment Sealer | S03-2410H, SW6-0909H New | Color base |
| Pigment Topcoat | B03-241025H, BWEx 01-0525H | Final color coat |
| TB Additive | TB | Increases hardness & chemical resistance (+2%) |

**Improvements:**

• [+]  **~20% cost savings** vs. solvent-based for the same color

• [+]  **High hiding power** — fast coverage, especially on MDF

• [+]  Can be thinned with Diluent BT-08H or Retarder BT-01H (slow drying)

• [TIME]  Drying time: **60-90 min** (sealer), **12-24h** (packaging)

4.2. Acrylic-Based Sealers & Topcoats

Anti-Grain-Raising Primer — BT-1025H

• [+]  **Minimizes grain raising** on susceptible wood species (oak, rubberwood, pine)

• [+]  Use when a **bright, clear** finish is needed — base layer for stain systems

• [TIME]  Drying time: **40-60 min**

Clear Sealer — S07-2706H

• [+]  **Excellent clarity** — comparable to NC

• [+]  Low viscosity → **deep penetration**, fills grain pores

• [+]  Dilute 3-5% with Diluent BT-08H or Retarder BT-01H

• [TIME]  Drying time: **40-60 min**

Adhesion-Enhancing Sealer — S04-0425 TB H

• [+]  **Improves adhesion** of water-based coatings over NC/PU sealers (hybrid systems)

• [TIME]  Drying time: **40-60 min**

Clear Topcoat — B03-241025H

• [+]  **Good clarity, NC-equivalent**

• [+]  Dilute 3-5% with Diluent/Retarder

• [+]  Can be tinted with pigment colors (<20%) for solid color applications

4.3. Hybrid Process — NC + Water-Based

This process combines the best of both systems:

| Step | Task | Product | Drying Time |
| --- | --- | --- | --- |
| 1 | Stain on raw wood | Stain Resin BT-1023 + Color | 20-30 min |
| 2 | NC Sealer | NC Sealer T2012 / HB | Per NC spec |
| 3 | WB Adhesion Sealer | S04-0425 TB H | 40-60 min |
| 4 | Stain over sealer | Stain Resin 1604H + Color | 20-30 min |
| 5 | WB Topcoat | B03-241025H | 12-24h packaging |

**Benefit:** The initial NC layer locks the wood grain → no grain raising, while the WB top layers provide non-yellowing, chemical-resistant performance.

4.4. Detailed Comparison Table

| Criterion | Traditional NC | WB Acrylic (BTChem) | WB PU (BTChem) |
| --- | --- | --- | --- |
| **Drying (oven 50°C)** | 15-20 min | **15-25 min** (comparable) | 20-30 min |
| **Drying (no oven)** | 20-30 min | 45-60 min | 60-90 min |
| **Film clarity** | ✅ Excellent | ✅ Good (improved, near NC) | ✅ Excellent |
| **Max gloss** | 80-90 GU | ✅ 80-90 GU | ✅ 90+ GU |
| **Hardness (Pencil)** | HB-F | F-H | ✅ **H-2H** |
| **Water resistance** | Poor | ✅ Good | ✅ ✅ Excellent |
| **Chemical resistance** | Poor | Fair (with TB additive) | ✅ ✅ Good |
| **Non-yellowing** | ❌ Yellows 6-12 months | ✅ Yellows much slower than NC | ✅ Non-yellowing |
| **Grain raising** | ✅ Minimal | ✅ Improved (with BT-1025H) | ✅ Good |
| **Application odor** | Strong, pungent | ✅ Very mild | ✅ Mild |
| **Fire safety** | Highly flammable | ✅ Low flammability risk | ✅ Low flammability risk |
| **Material efficiency** | Low (~30% solids) | ✅ ~20% savings vs NC | ✅ Efficient |
| **Cost** | Low | ✅ Nearly comparable | Higher |

4.5. Drying Technology — Practical Tips

| Technology | Speed | Advantage | Disadvantage |
| --- | --- | --- | --- |
| **Infrared (IR)** | ⚡ Very fast | Heats the substrate directly by radiation → heat conducts outward through the coating → moisture evaporates from the inside out, less "skin-over" | ⚠️ Shadows → slow drying → odor |
| **Convection** | Slower | Suitable for complex shapes | Risks "skin-over" if temperature too high |

**Practical drying tips:**

- Allow paint to **flash off completely** (5-15 min) before entering 50°C+ oven

- Ramp temperature gradually (40°C → 55°C) — prevents cracking, blistering, wrinkling

- With IR drying: pay attention to shaded areas — incomplete drying causes packaging odor

4.6. Dip Coating — Ideal for Water-Based

Water-based paints are well-suited for **dip (immersion) coating** technology:

• [+]  **Stable viscosity** when held in dip tanks — water evaporates more slowly than solvent, so viscosity remains consistent throughout the work shift

• [+]  **No hazardous solvent fumes** escaping into the work environment — safer for operators, no need for explosion-proof equipment

• [+]  **Reduced material waste** vs. hand spraying

• [+]  **Less dependent on operator skill**

• [+]  Suitable for natural wood components + MDF sheets (combine with roller coating)

• [!]  **Viscosity must be closely monitored** — WB dip tanks are prone to foaming and sagging if not properly controlled

────────────────────────────────────────────────────────────────────────────────

Part 5: KEY DIFFERENCES — WHAT PRODUCTION TEAMS MUST KNOW

5.1. DRYING — NOT the same as NC

| NC | Water-Based |
| --- | --- |
| Air dries naturally | Requires oven or extended time |
| Fast — 15-30 min | Slow — 30-60 min/coat |
| Weather-independent | **Highly sensitive to humidity & temperature** |
| Fast surface dry → easy multi-coat | Slow surface dry → dust pickup, sagging |

**Note:** WB **cannot dry as fast as NC** without an oven. Without an oven, slow down the line or extend the conveyor. Pay extra attention in humid weather.

👉 **BTChem solution:** Sealer S07-2706H + Topcoat B03-241025H with Diluent BT-08H and Retarder BT-01H for flexible drying control.

5.2. GRAIN RAISING — Water swells wood fibers

Water penetrates wood and swells the grain fibers. NC has no such issue since solvents don't swell wood.

**Solutions:**

• Sand **finer** than NC (use 320-400 grit)

• Apply **Anti-Grain-Raising Primer BT-1025H** — locks fibers, blocks water penetration

• After priming, allow extra drying time, sand thoroughly

👉 **With BT-1025H:** Grain raising is significantly reduced — smooth surface ready for stain or sealer.

5.3. SPRAYING — Different technique

| NC | Water-Based |
| --- | --- |
| Pressure: 30-40 psi | ⚡ Pressure: **25-30 psi** (lower) |
| Nozzle: 1.0-1.3mm | ⚡ Nozzle: **1.3-1.5mm or 2.5mm** (larger) |
| Can apply wet heavy coats | ⚡ **Avoid heavy wet coats** — sag, slow dry, bubbles |
| Spray edges first → faces last | ⚡ **Spray faces first → edges last** (slow surface dry) |
| Easy gun adjustment | ⚡ More difficult — bubbles, orange peel |

**Note:** For WB, **use a 2-pass technique** — first pass light (even dry), second pass wet on top. Never apply one heavy coat.

5.4. FOAMING — The enemy of water-based

WB easily **foams** and foam is **slow to dissipate**, causing surface roughness and pinholes.

**Causes:**

• High-speed / aggressive stirring

• Excessive spray air pressure

• Air sparging (never use to stir WB paint)

**Prevention:**

• Stir at moderate speed

• No air sparging

• Anti-settling agitator at low speed

• Spray at moderate pressure (25-30 psi)

5.5. COLOR MATCHING — Harder than NC

WB paint is milky-white when wet and becomes clear only when dry. This makes wet color matching difficult.

**Tips:**

• Learn the wet-to-dry color shift for your specific product

• Always evaluate color after complete drying

• Use stain colors specifically designed for water-based (solvent stains may appear washed out)

5.6. EQUIPMENT CLEANING — No thinner

| NC | Water-Based |
| --- | --- |
| Clean with **NC thinner** | ⚡ Clean with **clean water** or specialized solvent |
| Solvent or mineral spirits OK | **Never use thinner or mineral spirits** |

**Note:** Cleaning WB guns with solvent will cause paint coagulation and nozzle clogging. Clean immediately after use — do not let paint dry on equipment.

────────────────────────────────────────────────────────────────────────────────

Part 6: REQUIRED INVESTMENTS FOR CONVERSION

6.1. Mandatory Equipment

| Equipment | Why | Estimated Cost |
| --- | --- | --- |
| **Drying oven** | WB requires controlled drying | High |
| **Larger spray nozzle** | ≥1.3mm or 1.5mm nozzle | Low |
| **Low-speed agitator** | Prevents foaming | Low |
| **DIN4 viscosity cup** | WB viscosity measurement (different from DIN2 for NC) | Very low |

6.2. Recommended Equipment

| Equipment | Reason |
| --- | --- |
| **Wood moisture meter** | Control wood moisture → prevent grain raising and slow drying |
| **Laser surface thermometer** | Ensure wood surface isn't too hot before spraying |
| **Spray booth air filtration** | Reduce dust — WB dries slowly so dust settles easily |
| **IR oven** | Fast surface drying — watch shaded areas |

6.3. Personnel Training

• Retrain spray operators** — minimum 1-2 weeks

• Assign a process control person** to monitor viscosity, temperature, humidity during each shift

• Color matchers need re-training** — WB color behaves differently from NC

────────────────────────────────────────────────────────────────────────────────

Part 7: TECHNICAL DIFFERENCES TO NOTE

7.1. Temperature & Humidity

WB is highly sensitive to weather:

| Condition | Effect on WB Coating |
| --- | --- |
| **Ideal temperature** | 20–30°C (local workshop conditions in Vietnam typically 28–35°C — acceptable but monitor closely above 32°C) |
| **Ideal humidity** | <70% |
| **High humidity (rainy)** | ⚠️ Very slow drying, white spots, mold risk |
| **Hot, dry weather** | ⚠️ Flash-off too fast → wrinkling, orange peel |
| **Hot wood surface (>40°C)** | ⚠️ Sudden drying, cracking, embrittlement |

**Solution:** Without an oven, monitor weather before production. At >80% humidity, slow down or stop WB production.

7.2. Viscosity — Measured differently

| System | Cup | Typical Production Viscosity |
| --- | --- | --- |
| **NC** | DIN2 (#2 cup) | 15-20 sec |
| **WB** | **DIN4** (#4 cup, equivalent to Ford #4 / ISO 2431 ø4mm) | 25-40 sec |

**Note:** WB viscosity is **unstable** — just a small amount of water/diluent can cause a sharp drop. Add gradually (5% increments) and re-measure after each addition.

7.3. Packaging — Watch for odor and sticking

If WB is **not fully dry** at packaging:

• [-]  Surface sticking, packaging adhesion

• [-]  Residual odor (trapped water and chemicals)

• [-]  Especially in shaded areas and back surfaces

**Check:** Press a finger into the coated surface — if a fingerprint remains or the film feels soft, do not package yet.

7.4. Rework — Different from NC

NC rework is straightforward: sand and recoat. WB rework is more challenging:

• Sand **more thoroughly** before recoating

• Severe defects may require **full stripping** before rework

• Reworked WB is more prone to grain raising

7.5. Stain/Color — Use the right type

| Type | NC | Water-Based |
| --- | --- | --- |
| **Solvent-based stain** | ✅ Works | ⚠️ Color fades/washes out when water is applied |
| **Water-based stain** | Works but not optimal | ✅ Works best |

**Note:** If using solvent stain under WB, mix with stain resin or incorporate into sealer/topcoat to prevent color shift.

────────────────────────────────────────────────────────────────────────────────

Part 8: CONVERSION CHECKLIST — NC → WATER-BASED

☐ Equipment

☐ **Drying oven** available? Maximum temperature?

☐ Conveyor **long enough** for required drying time?

☐ **Spray nozzle** upgraded to ≥1.3mm?

☐ **DIN4 cup** available for viscosity measurement?

☐ Agitator set to **low speed**?

☐ Environment

☐ Spray area temperature ideally ≤30°C? (≤35°C acceptable for Vietnam conditions — monitor closely)

☐ Production plan for rainy/humid days?

☐ Spray booth clean (dust-free)?

☐ Materials

☐ **Anti-grain-raising primer** in stock (BT-1025H)?

☐ **Water-based stains/colors** ready?

☐ **Diluent/Reducer** for WB available?

☐ Personnel

☐ Spray operators trained on WB technique?

☐ Color matchers experienced with WB?

☐ QC team aware of common WB defects and inspection methods?

☐ Process

☐ Trial runs completed to determine actual drying time?

☐ Conveyor speed adjusted for WB?

☐ In-process viscosity check procedure established?

────────────────────────────────────────────────────────────────────────────────

Part 9: COMMON CONVERSION DEFECTS

| Defect | Cause | Solution |
| --- | --- | --- |
| **Grain raising** | Water penetrates wood fibers | Anti-grain primer, fine sanding, thorough drying |
| **Foaming** | High spray pressure, aggressive stirring | Reduce pressure, stir gently, no air sparging |
| **Slow drying** | High humidity, low temp, no oven | Oven dry, reduce line speed, increase spacing |
| **Orange peel** | Paint too thick, wrong nozzle | Thin properly, use larger nozzle, correct pressure |
| **Sagging** | Over-wet application, too much paint | Reduce paint volume, use 2 thin passes |
| **Uneven color** | Uneven film thickness, wet/dry color shift | Even application strokes, learn color shift |
| **Packaging adhesion** | Incomplete drying | Extend drying time, check before packaging |
| **Packaging odor** | Shaded areas not fully dried | Monitor hidden areas during drying, extend air-dry time |
| **Uneven gloss** | Uneven surface, inconsistent paint | Uniform sanding, thorough mixing, even spraying |
| **Cracking** | Paint too thick, oven too hot | Thinner coats, ramp oven temperature gradually |

────────────────────────────────────────────────────────────────────────────────

SUMMARY

| Aspect | NC Solvent-Based | Water-Based |
| --- | --- | --- |
| Ease of application | ✅ Easy | ⚠️ More challenging, training needed |
| Material cost | ✅ Lower | ✅ Nearly comparable |
| Equipment cost | ✅ Low | Requires oven investment |
| Film quality | Fair | ✅ Superior |
| Worker health | Poor | ✅ Safe |
| Environmental | Poor | ✅ Green |
| Export compliance | Limited | ✅ Meets international standards |

**Recommendation:**

- For **low-cost, low-volume, no-oven** production → stick with NC

- For **export-grade, high-quality production with oven** → invest in water-based

- **Hybrid approach:** NC as primer (anti-grain-raising), WB as topcoat — or vice versa depending on the product

────────────────────────────────────────────────────────────────────────────────

*Document compiled from BTChem (Hóa Keo Bình Thạnh) internal technical training materials and production experience.*

*Author: Ngô Đức Minh — Technical Department*