TECHNICAL DATA SHEET

Product:  COATING 2706 H

Date: 29/07/2026

## DESCRIPTION

Water-based coating for interior wooden products, environmentally friendly.

## CHARACTERISTICS

• Easy to apply — suitable for dipping or spraying methods

• Fast penetration into wood surface, quick drying, good water resistance

## TECHNICAL SPECIFICATIONS

| Parameter | Value |
| --- | --- |
| Appearance | Milky white liquid |
| Viscosity (~30°C) | 19–21 seconds (Din 4) after dilution with Thinner 2706 H |
| Drying time (room temp. 30–35°C): |  |
| – Dust-free | 15–20 minutes |
| – Packaging-ready | 5–6 hours |
| Shelf life | 6 months in cool, ventilated storage. Keep lid tightly closed before and after use. Stir well before use. |
| Note | Stir the coating thoroughly before and during use. |

## MIXING RATIO

| Component | Ratio |
| --- | --- |
| Pallet Coating 2706 H | 4 |
| Thinner 2706 H | 1 |

## GENERAL PROCEDURE

Surface preparation: Remove all defects from the wood surface. Sand with #240 sandpaper. Clean and dry thoroughly. Moisture content < 12%.

Process: Dip the product into the Pallet Coating 2706 H mixture.

Note: Specific detailed procedures may apply depending on the actual case.

## EQUIPMENT

• Spray booth must be placed in a well-ventilated area, free from dust

• Coating system must be equipped with ventilation fans and dust/solvent vapor extractors

• The spray booth should be fitted with heating/drying lamps to cure products at 30–35°C

## SAFETY AND STORAGE

• Avoid contact with eyes, skin, and mouth. Provide workers with masks, gloves, and protective gear.

• Coating components are flammable chemicals — keep away from heat, sparks, and open flames.

• Store paint containers in a cool, ventilated area. Keep containers tightly closed before and after use.