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DESCRIPTION
Water-based coating for interior wooden products, environmentally friendly.
CHARACTERISTICS
• Easy to apply — suitable for dipping or spraying methods
• Fast penetration into wood surface, quick drying, good water resistance
TECHNICAL SPECIFICATIONS
	Parameter
	Value

	Appearance
	Milky white liquid

	Viscosity (~30°C)
	19–21 seconds (Din 4) after dilution with Thinner 2706 H

	Drying time (room temp. 30–35°C):
	

	   – Dust-free
	15–20 minutes

	   – Packaging-ready
	5–6 hours

	Shelf life
	6 months in cool, ventilated storage. Keep lid tightly closed before and after use. Stir well before use.

	Note
	Stir the coating thoroughly before and during use.



MIXING RATIO
	Component
	Ratio

	Pallet Coating 2706 H
	4

	Thinner 2706 H
	1



GENERAL PROCEDURE
Surface preparation: Remove all defects from the wood surface. Sand with #240 sandpaper. Clean and dry thoroughly. Moisture content < 12%.
Process: Dip the product into the Pallet Coating 2706 H mixture.
Note: Specific detailed procedures may apply depending on the actual case.
EQUIPMENT
• Spray booth must be placed in a well-ventilated area, free from dust
• Coating system must be equipped with ventilation fans and dust/solvent vapor extractors
• The spray booth should be fitted with heating/drying lamps to cure products at 30–35°C
SAFETY AND STORAGE
• Avoid contact with eyes, skin, and mouth. Provide workers with masks, gloves, and protective gear.
• Coating components are flammable chemicals — keep away from heat, sparks, and open flames.
• Store paint containers in a cool, ventilated area. Keep containers tightly closed before and after use.
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