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Disclaimer: These indicators above were tested under certain condition, not guaranteed for all usage. For different
application and using condition, formula validation is needed, to ensure that the product meets the requirement.
Dipentaerythritol
i
D pentaerythritol Hexaacrylate
exaacrylate
DPHA-80
Product specifications：
Items
Specification
Testing methods
Appearance
Slightly mixed
until transparent
liquid
Visual inspection
Color（APHA）
≤100
GB/T 3143-1982
(Platinum-Cobalt Method)
Viscosity（cps/25℃）
3000-10000
GB/T 2794-2013
Acid Value（mgKOH/g）
<1.0
GB/T 6743-2008
Specific Gravity（g/cm3）
1.20±0.02
GB/T 6750-2007
Refractive Index（25℃）
1.484±0.005
GB/T 614-2006
Functionality
5.5
Theoretical values
Effective Constituent（%）
100
Theoretical values
Characteritics：

Medium viscosity

Fast curing speed

High sensitivity

High hardness

High wear resistance
Applications：

PCB ink

UV offset ink

Hardening fluid

Plastic UV coating

PVC plus hard paint
Shelf life：
Store at room temperature sealed away from light, shelf life: 12 months.
Packaging：
25L Packing Drum & 200L Packing Drum.




