DPHA-80 — Dipentaerythritol Hexaacrylate

Guangdong Bossin Novel Materials Technology Co., Ltd.

Guangdong Bossin Novel Materials Technology Co., Ltd.

Add: No.8 Haicheng East Street, Xingang East Road, Haizhu District, Guangzhou, Guangdong，China

Tel：+86 20 34379001

Fax：+86 20 34379190

Web：www.gzbossin.com

Ver：2025.04

Disclaimer: These indicators above were tested under certain condition, not guaranteed for all usage. For different

application and using condition, formula validation is needed, to ensure that the product meets the requirement.

Dipentaerythritol

i

D pentaerythritol Hexaacrylate

exaacrylate

DPHA-80

Product specifications：

Items

Specification

Testing methods

Appearance

Slightly mixed

until transparent

liquid

Visual inspection

Color（APHA）

≤100

GB/T 3143-1982

(Platinum-Cobalt Method)

Viscosity（cps/25℃）

3000-10000

GB/T 2794-2013

Acid Value（mgKOH/g）

<1.0

GB/T 6743-2008

Specific Gravity（g/cm3）

1.20±0.02

GB/T 6750-2007

Refractive Index（25℃）

1.484±0.005

GB/T 614-2006

Functionality

5.5

Theoretical values

Effective Constituent（%）

100

Theoretical values

Characteritics：



Medium viscosity



Fast curing speed



High sensitivity



High hardness



High wear resistance

Applications：



PCB ink



UV offset ink



Hardening fluid



Plastic UV coating



PVC plus hard paint

Shelf life：

Store at room temperature sealed away from light, shelf life: 12 months.

Packaging：

25L Packing Drum & 200L Packing Drum.