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Disclaimer: These indicators above were tested under certain condition, not guaranteed for all usage. For different
application and using condition, formula validation is needed, to ensure that the product meets the requirement.
Dipentaerythritol
Dipentaerythritol Hexaacrylate
exaacrylate
DPHA-90
Product specifications：
Items
Specification
Testing methods
Appearance
Clear liquid
Visual inspection
Color（APHA）
≤60
GB/T 3143-1982
(Platinum-Cobalt Method)
Viscosity（cps/25℃）
4000-8000
GB/T 2794-2022
Acid Value（mgKOH/g）
≤0.5
GB/T 6743-2008
Specific Gravity（g/cm3）
1.20±0.02
GB/T 6750-2007
Refractive Index（25℃）
1.487±0.005
GB/T 614-2006
Functionality
6
Theoretical values
Effective Constituent（%）
100
Theoretical values
Characteritics：

Synthesized from 90 grade dipentaerythritol

Low impurity content & Fast curing speed

High cross-linking density & High hardness and wear resistance
Applications：

UV plus hard liquid & PVC plus hard paint

PCB ink & UV offset ink & Plastic UV coating
Shelf life：
Store at room temperature sealed away from light, shelf life: 12
months.
Packaging：
25L Packing Drum & 200L Packing Drum.
Notes：
Due to the molecular structure characteristics, BM6263 may crystallize
or turn white during long-term storage at low temperatures. It can be
restored to a transparent and uniform state through heat treatment (40-60℃,
held for 24 hours or more).




