DPHA-90 — Dipentaerythritol Hexaacrylate

Guangdong Bossin Novel Materials Technology Co., Ltd.

Guangdong Bossin Novel Materials Technology Co., Ltd.

Add: No.8 Haicheng East Street, Xingang East Road, Haizhu District, Guangzhou, Guangdong，China

Tel：+86 20 34379001

Fax：+86 20 34379190

Web：www.gzbossin.com

Ver：2026.03

Disclaimer: These indicators above were tested under certain condition, not guaranteed for all usage. For different

application and using condition, formula validation is needed, to ensure that the product meets the requirement.

Dipentaerythritol

Dipentaerythritol Hexaacrylate

exaacrylate

DPHA-90

Product specifications：

Items

Specification

Testing methods

Appearance

Clear liquid

Visual inspection

Color（APHA）

≤60

GB/T 3143-1982

(Platinum-Cobalt Method)

Viscosity（cps/25℃）

4000-8000

GB/T 2794-2022

Acid Value（mgKOH/g）

≤0.5

GB/T 6743-2008

Specific Gravity（g/cm3）

1.20±0.02

GB/T 6750-2007

Refractive Index（25℃）

1.487±0.005

GB/T 614-2006

Functionality

6

Theoretical values

Effective Constituent（%）

100

Theoretical values

Characteritics：



Synthesized from 90 grade dipentaerythritol



Low impurity content & Fast curing speed



High cross-linking density & High hardness and wear resistance

Applications：



UV plus hard liquid & PVC plus hard paint



PCB ink & UV offset ink & Plastic UV coating

Shelf life：

Store at room temperature sealed away from light, shelf life: 12

months.

Packaging：

25L Packing Drum & 200L Packing Drum.

Notes：

Due to the molecular structure characteristics, BM6263 may crystallize

or turn white during long-term storage at low temperatures. It can be

restored to a transparent and uniform state through heat treatment (40-60℃,

held for 24 hours or more).