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Feature:
SW107
Low odor Acrylic Monomer

High hardness, high brittleness, good yellowing, good adhesion, less odor than HEMA, does not irritate the skin.
No skin irritation even when heated, no HEA, HPA, volatile gases are basically non-irritating to the eyes.
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	Range

	Appearance
	Colorless clear liquid

	Functionality
	2

	Colour(APHA)
	25Max

	TG(℃）
	65

	Viscosity(cps at 25 ℃)
	5-10


Usage:
1, Curing faster than HEMA more than 1 times for UV thinning agent 
2, AB adhesive; not recommended for synthetic
Storage and transportation:
Please keep it away from heat source and put it in the shadow place, and store it in room temperature for 12 months without deterioration. 
Wrap:25/200KG/drum   Brand:Wangsan
      

Address：NO.1 301 Hong bafang investment BLDG1.Guan chong village Shiqi town Panyu district ,Guangzhou
TEL：86-20-82562016              FAX：86-20-31078112
Website：http://www.swanchemical.com 
E-mail:admin@gzwangsanchem.com
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