SW107

Low odor Acrylic Monomer

Feature:

High hardness, high brittleness, good yellowing, good adhesion, less odor than HEMA, does not irritate the skin.

No skin irritation even when heated, no HEA, HPA, volatile gases are basically non-irritating to the eyes.

Specification:

| Index | Range |
| --- | --- |
| Appearance | Colorless clear liquid |
| Functionality | 2 |
| Colour(APHA) | 25Max |
| TG(℃） | 65 |
| Viscosity(cps at 25 ℃) | 5-10 |

Usage:

1, Curing faster than HEMA more than 1 times for UV thinning agent

2, AB adhesive; not recommended for synthetic

Storage and transportation:

Please keep it away from heat source and put it in the shadow place, and store it in room temperature for 12 months without deterioration.

Wrap:25/200KG/drum   Brand:Wangsan